**1060铝板**具有延伸率高，抗拉强度大，导电性优良，成型行高的有点，完全能够满足常规的加工（冲压，拉伸）要求。1060铝板具有良好的高耐腐蚀性，导电导热性能和可焊接性。薄板多用于汽车零部件，电池软连接，幕墙板，大巴行李架，地板和花纹板等。厚板多用于铝母线，汽车散热器，新能源汽车充电桩，模具等。

1060 aluminum sheet & plate has high elongation, high tensile strength, excellent electrical conductivity, and high forming line, which can fully meet the conventional processing (stamping, stretching) requirements. 1060 aluminum sheet & plate has good high corrosion resistance, electrical and thermal conductivity and weldability. Thin sheet is mostly used in auto parts, battery soft connections, curtain wall panels, bus luggage racks, floor and pattern plate. Thick plate is mostly used in aluminum buses, automobile radiators, new energy automobile charging piles, mold and so on.

**应用：**

1、1060铝板薄板多用于汽车零部件，电池软连接，幕墙板，大巴行李架，地板和花纹板等。

2、1060铝板厚板多用于铝母线，汽车散热器，新能源汽车充电桩，模具等。

Application:  
1, 1060 aluminum sheet is mostly used in auto parts, battery soft connections, curtain wall panels, bus luggage rack, floor and pattern plate.  
2, 1060 aluminum plate is mostly used in aluminum buses, automobiles radiator, new energy vehicle charging pile, mold and so on.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 合金  ALLOY | 状态  TEMPER | 厚度  GAUGE | 宽度  WIDTH | 长度  LENGTH |
| 1060 | O, F，H12，H14、H16、H18、H19、H22、H24、H26、H28，H112,etc | 0.1-500mm  0.0039”-19.685” | 20-2650mm  0.7874”-104.331” | 500-16000mm  19.685”-629.921” |