**3005铝板**是Al-Mn合金的一种，强度比3003铝板高20%左右，耐蚀也更好。又可称为防锈铝板，广泛用于百叶窗料、灯头料、宽幅幕墙板，彩图铝基板等。

3005 aluminum sheet & plate is a kind of Al-Mn alloy, the strength is about 20% higher than 3003 aluminum sheet & plate, and the corrosion resistance is also better. It can also be called rust-proof aluminum plate, which is widely used in shutter material, lamp cap material, wide screen wall panel, color aluminum substrate and so on.

**应用：**

1、3005铝板广泛用于百叶窗料、灯头料、宽幅幕墙板，彩图铝基板等。

Applications:
1, 3005 aluminum plate is widely used in shutter material, lamp cap material, wide screen wall panel, color aluminum substrate and so on.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| 合金ALLOY | 状态TEMPER | 厚度GAUGE | 宽度WIDTH | 长度LENGTH |
| 3005 | O, F，H12，H14、H16、H18、H19、H22、H24、H26、H28，H112,etc | 0.1-500mm0.0039”-19.685” | 100-2650mm3.937”-104.331” | 500-16000mm19.685”-629.921” |