**仿石纹彩涂铝板**是在铝板表面经铬化等预处理后进行氟碳辊涂布而成的印刷产品。它已成为取代传统石材和玻璃幕墙的新材料。  
The faux stone pattern coated aluminum sheet is a printed product created by roller-coating with fluorocarbon after the aluminum sheet undergoes pretreatment such as chromization. It has become a new material replacing traditional stone and glass curtain walls.

**应用：**

1、广泛应用于机场、火车站、写字楼、商场、酒店、酒吧、会所、美术馆、博物馆墙面等。

Applications:  
1, Widely used in airports, train stations, office buildings, shopping malls, hotels, bars, clubs, art galleries, museums, and other wall surfaces.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 合金  ALLOY | 状态  TEMPER | 涂层厚度  COATING GAUGE | 厚度  GAUGE | 宽度  WIDTH | 长度  LENGTH |
| 1050/1060/1100or as per customer’s requests | H24 or as per customer’s requests | As per customer’s requests | 0.25-1.35mm  0.0098“-0.0531” | 30-1350mm  1.1811“-53.15” | 2000-6000 mm  78.74“-236.22” |